## Slide 1: Silicones for Home and Car Care
BRB International B.V.
2 July 2018
Version 3.1

## Slide 2: What are we going to discuss?
Car Care Surface Care
Wash and Rinse Aid
Exterior Car polish
Windscreen & glass cleaners
Tire/Rim Care
Interior Trim/Dashboard
Exterior Trim
Leather conditioners
Home Care Surface Care
Furniture and wood polishes
Floor polish
Metal/stainless steel polish
Shoe & Leather care
Glass cleaners
Carpet cleaning products
Tile grout sealers
Antistatic solutions
Home Care Laundry Care
Laundry detergents additives
Fabric softeners additives
Dry cleaning

## Slide 3: Characteristics of silicones
CHARACTERISTIC
Low surface tension
Strong Si-O & Si-C bonds
High R.I:(1.375 -1.403)
Low intermolecular forces
(high chain flexibility)
Methyl groups
Low Glass Transition
BENEFIT
Spreads on most surfaces
UV, oxidative, thermal &
chemical stability
Gloss
Lubricity & high permeability,
low surface friction
Water repellency
Liquids at high molecular weight

## Slide 4: Why use silicones in Car&Home Care?
Ease of application - lubricant
Polish cleaning ability - increase surface wettability
Ease of polishing - lubricant, less effort to polish
Streakability - reduces “streaking” of polish
Gloss / Shine – high Refractive Index
Increase colour intensity (depth of gloss)
Surface protection - durability & detergent resistance
Water repellency – long lasting
Surface smoothness/slip – more difficult for dirt to adhere

## Slide 5: What is a polish?
Polish = a temporary coating that enhances and protects the substrate to which it is applied.
Enhances by cleaning and increasing gloss/color intensity.
Protects by depositing a barrier film that repels water and gives a degree of dirt repellency.
A polish does not have to come in a form of a paste or gel. It can also be in the form of a sprayable liquid.

## Slide 6: Car Care – Surface Care
Wash & Rinse Aids
Exterior Polishes & Waxes
Windscreen & Glass Cleaners
Tire/Rim Care
Interior Trim/Dashboard Care
Exterior Trim Care
Leather Care

## Slide 7: Home Care – Surface Care
Furniture and wood polishes
Floor polish
Metal/stainless steel polish
Shoe & Leather care
Glass cleaners
Carpet cleaning products
Tile grout sealers
Antistatic solutions

## Slide 8: Home&Car Care – consumer requirements
Ease of use
Enhancement of color, gloss
Lasting protection
Water repellency
Dirt repellency
Self-cleaning or easy re-cleaning ability

## Slide 9: Silicones for the Home&Car Care Industry
Silicone Oils
BRB Silicone Oils 50, 350, 1000, 12.500, 60.000 cSt
Silicone Emulsions
BRB Sempure 35, BRB Sempure 60, BRB Sempure 66
BRB Sempure HV 6500, BRB Sempure 1997
Aminofunctional Oils
BRB SF 230 NEW, BRB SF 240, BRB SF 315 NEW, BRB SF 430
Aminofunctional Emulsions
BRB Sempure 3733, BRB Sempure 135, BRB Sempure 152 NEW, BRB Sempure 230
Specialty Emulsions
BRB Sempure 330 NEW, BRB Sempure 422 NEW

## Slide 10: Silicones for the Home&Car Care Industry - continued
Volatile Silicones
BRB CM 40, BRB CM 50, BRB Silicone oil 0,65 cst
Silicone Glycols
BRB 526, BRB 6373, BRB 431
Silicone resins
  BRB TMS, BRB TMS-50I, BRB TMS-50C
Paintable Silicones
BRB Sempure 5332, BRB Alkyl Aryl Fluid
Silicone antifoams
BRB Akasil TG 10/20/30, BRB Akasil RE 20

## Slide 11: Silicone oils & emulsions - range
BRB Sempure 35 & 60
35% or 60% non-ionic emulsion of mid viscosity PDMS for general purpose polish formulations.
BRB Sempure 66
60% non-ionic emulsion of low viscosity PDMS for general purpose polish formulations. Great spreadability and ease of use.
BRB Sempure HV 6500
60% non-ionic emulsion of high & low viscosity PDMS blend for premium polish formulations. Optimized balance between ease of application, spreading, gloss & durability.
BRB Sempure 1997
55% non-ionic emulsion of high viscosity PDMS for superior shine and long durability
BRB Silicone oils 50, 350, 1.000, 12.500, 60.000 cSt
For customers who want to emulsify by themselves and fine tune their own emulsions

## Slide 12: Silicone oils & emulsions - benefits
Ease of application – streak & smear resistant
Improved cleaning - low surface tension, increases surface wetting.
Depth of Gloss / Color – high Refractive Index
Water repellency – presence of methyl groups promotes water beading
Slip - gives a smooth/lower friction surface

## Slide 13: Silicone oils & emulsions – applications
Rubber, vinyl, plastic and leather protectants
Furniture cleaners and protectants
Hard surface cleaners and protectants
Spray and wipe polishes (quick detailers)
Car shampoos
Paint polishes, waxes and sealants
Dosage of silicone emulsion(s) in the formulation depends on the type of emulsion and the type of formulation. It can vary from 5% to 35%.
Dosage of silicone oil(s) varies from 1% to 15%.

## Slide 14: Silicone Oils - formulating
Formulation properties
Oil soluble, not water soluble
Medium viscosity: easier application & emulsification
Higher viscosity: better protection & conditioning
Defoaming properties
Can be formulated into
Solvent in water emulsions, normally use 50-1000 cSt PDMS
Water in solvent - can include high visc fluids
Polish formulations - use a combination of high/medium viscosity fluids to optimize benefits
Viscosity | 100 / 350 | 1000 | 12.500 / 60.000
Ratio | 3 | 1 | 1
Benefit | Ease of use | Gloss | Durability

## Slide 15: Silicone Oils – optimization of properties
Viscosity | Gloss | Durability / Protection | Wetting / Spreading | Overall ease of use
PDMS(50cs) |  |  |  | 
PDMS(350cs) |  |  |  | 
PDMS(1000cs) |  |  |  | 
PDMS(12500cs) |  |  |  | 
PDMS(60000cs) |  |  |  | 

## Slide 16: Aminofunctional silicones - properties
Dimethicone backbone grafted with amino groups
Polar amine groups effectively anchor the product to substrate -> physical attraction to negatively charged surfaces
Reactive grades crosslink to form a polymer film with high detergent resistance and effective protection

## Slide 17: Aminofunctional oils - range
 |  | Viscosity at 25°C (cSt) | Nitrogen content (%w/w)
BRB SF 230 |  | 3000 | 0.2
BRB SF 240 |  | 4000 | 0.2
BRB SF 315 |  | 1500 | 0.3
BRB SF 430 |  | 3000 | 0.4

## Slide 18: Aminofunctional oils – properties
Characteristic |  | 
Viscosity | Low | High
Amine Content | Low | High
Durability |  | 
Hydrophobicity |  | 
Gloss |  | 

## Slide 19: Aminofunctional emulsions - range
BRB Sempure 3733
40% cationic macro emulsion for extended durability and slip.
BRB Sempure 135
35% non-ionic micro emulsion for extended durability and good hydrophobic effect. Allows to formulate transparent products.
BRB Sempure 152
50% non-ionic macro emulsion of aminofunctional silicone polymer. For extraordinary softness.
BRB Sempure 230
30% non-ionic micro emulsion of silicone quaternium polymer. Film former. Allows to formulate transparent products.

## Slide 20: BRB Sempure 135 – for Car Care
Properties
  35% active, micro emulsion of aminofunctional silicone
  Specifically developed for use in transparent, aqueous, hard surface cleaning & conditioning products
  Forms a protective layer on the treated surface to provide water repellency, increased gloss and durable protection.
Benefits
  Easy to formulate into aqueous systems
  Remains transparent in most detergent formulations
  Beads-up water on surfaces
  Small particle size preventing residual smearing on the glass
  Imparts water repellency, increased gloss and durable protection
  Good slippery effect
Typical dosage: 1,0-10%.

## Slide 21: BRB Sempure 152 – new for Car & Home Care
Properties
  52% active, macro-emulsion of aminofunctional silicone
  Specifically developed for soft touch effect
  Little to no yellowing on fabrics
Benefits
  Provides outstanding softness to fabric and leather
  Provides good hydrophobic effect, increased gloss and durable protection on hard surfaces
  Compatible with esterquats
  Easy to formulate into aqueous blends
Typical dosage: 1-5%.

## Slide 22: BRB Sempure 230 – for Home Care
Properties
  30% active, micro-emulsion of silicone quaternium polymer
  Specifically developed for cleaning formulations
  Offers shine and protection to ceramics, glass and painted surfaces
Benefits
  Hydrophobising film former
  Reduces formation of streaks and scale on tiles and glass
  Increases the durability of water based polishes
  Easy to formulate into aqueous blends
  Can be formulated in transparent products
  Can also be used in car care formulations
Typical dosage: 0,5-2,5%.

## Slide 23: Aminofunctional Silicones - benefits
Ease of application – streak resistant
Depth of Gloss / Color – high Refractive Index
Strong hydrophobic effect – water beading
Durability - semi-permanent bonding to the substrate
Slip - give a smooth/lower friction surface
Dirt repellency/easy cleaning – due to smooth, hydrophobic surface

## Slide 24: Aminofunctional Silicones - applications
Rubber, vinyl, plastic and leather protectants – in combination with base silicone emulsions, dosage up to 5%
Furniture and hard surface protectants – dosage up to 3%
Glass cleaners and windscreen washers – dosage up to 1%
Spray and wipe polishes (quick detailers) – in combination with base silicone emulsions, dosage up to 3%
Spray waxes and sealants – Sempure 135, dosage up to 10%
Car shampoos – Sempure 135, dosage up to 5%
Paint polishes and waxes – dosage up to 10%

## Slide 25: Specialty emulsions
BRB Sempure 330 - is a 30% active emulsion of a high molecular weight silicone urethane resin. It is used to improve water repellency, dirt resistance, gloss and softness in various formulations of hard surface and leather dressings. It provides long-lasting protection to a treated surface.
BRB Sempure 422 - is a 22% active microemulsion of phenyl functional silicone and a quaternary ammonium functional silicone. It combines the gloss-boosting effect of phenyl-modified silicone with film-forming properties of silicone quat allowing formulation of transparent products with unique properties. It is an alternative to classic gloss increasing emulsions of high viscosity silicone oils.

## Slide 26: BRB Sempure 330
Properties
  A 30% active emulsion of a high molecular weight silicone urethane resin
  Non-ionic emulsifier system
  Specifically developed for lasting protection
Benefits
  Hydrophobising film former
  Very good durability and resistance to elements
  Gloss improvement and streak free finish
  Especially suitable for leather protection
  Easy to formulate into aqueous blends
Typical dosage: 0,5-5,0%.

## Slide 27: BRB Sempure 422
Properties
  22% active, micro-emulsion of phenyl modified silicone and silicone quaternium polymer
  Non-ionic emulsifier system
  Preservative free
Benefits
  Imparts excellent gloss enhancing benefits
  Imparts slickness to a treated surface
  Improves wipe-off with „no streak” effect
  Easy to formulate into aqueous blends
  Can be formulated in transparent products
Typical dosage: 1,0-5,0%.

## Slide 28: Volatile Fluids - range
BRB CM 50
Cyclopentasiloxane, D5
BRB CM 40
Cyclotetrasiloxane, D4
BRB Silicone oil 0.65cSt
Hexamethyldisiloxane

## Slide 29: Volatile Fluids - benefits
Oil and alcohol solubility
Volatile
Non-greasy
Good spreadability/wetting
Leaves no residue
Colorless/odorless
Safe for most common surfaces

## Slide 30: Volatile Fluids - applications
Polishes - replace solvents as carriers (for „solventless” solvent formulations)
Rinse and drying aids
Car waxes and sealants

## Slide 31: Silicone Glycols - range
BRB 526
PEG-12 Dimethicone
Emulsifier Si/W HLB 13
BRB 6373
Cyclopentasiloxane (and) PEG/PPG-18/18 Dimethicone
Emulsifier W/Si HLB 2
BRB 431
Modified trisiloxane
Superspreader, surface tension depressant

## Slide 32: BRB 526 – classic silicone glycol
Properties
Silicone surfactant based on ethoxylated dimethicone
Good wetting and surface tension reduction
Water soluble
Benefits
Improves spreading
Antifogging and sheeting properties
Reduces surface tension
Can also be used in car care formulations

## Slide 33: BRB 431 – trisiloxane superspreader
Properties
Superspreading surfactant based on trisiloxane ethoxylate
Outstanding surface tension reduction
Water soluble
Benefits
Improves spray coverage
Excellent penetration, antifogging and sheeting properties
Reduces surface tension already at very low level (0,1%)
Can also be used in car care formulations

## Slide 34: Silicone Glycols - benefits
Foam booster / foam quality
Water/alcohol dispersible
Spreading, wetting agents
Antifogging
Emulsifiers, dispersing agents

## Slide 35: Silicone Glycols - applications
Designed for formulating stable water in silicone emulsions or emulsions in which volatile silicones make up the oil phase. Emulsions based on silicone glycols are less greasy than typical water in oil products.
Cleaners with antifogging properties
Spreading additives in sprayable formulations

## Slide 36: Silicone Resins - range
BRB TMS
Trimethylsiloxysilicate in powder form
BRB TMS-50I
50% dispersion of Trimethylsiloxysilicate in Isododecane
BRB TMS-50C
50% dispersion of Trimethylsiloxysilicate in Cyclopentasiloxane

## Slide 37: Silicone Resins- benefits
Excellent film formers
Wash-off and rub-off resistant
Extraordinary water resistance
Great durability

## Slide 38: Silicone Resins - applications
Leather protectants (shoes, upholstery, etc.)
Exterior plastic and vinyl protectants
Car waxes and sealants

## Slide 39: Paintable Silicones
These silicones are capable of being over-painted. They do not require unusual or extraordinary cleaning operations prior to painting, plating or bonding. They are used in professional polishes in car body shops or custom paint shops.
BRB Sempure 5332
Paintable 50% non-ionic emulsion of alkyl aryl silicone
BRB Alkyl Aryl Fluid
For customers who want to emulsify by themselves
Also volatile fluids are over-paintable:
BRB CM 40
BRB CM 50
BRB Silicone oil 0.65 cst

## Slide 40: Silicone Antifoams
BRB Akasil TG 10, 20, 30
  Standard grade, silicone based antifoam emulsions
  Suitable for various home care applications
  Suitable for products with high salinity
  Good high temperature performance
  TG 10 : 14% active content
  TG 20 : 22% active content
  TG 30 : 30% active content
BRB Akasil RE 20
  Alkali resistant, silicone based antifoam emulsion
  Specifically developed for technical applications and to be used in a broad pH range
  Good high temperature performance
  Excellent knockdown as well as defoaming performance
  30 % active content

## Slide 41: Car Care - Product selector guide
 | Water based | Solvent based | Wash and Rinse Aid | Exterior car polish/ conditioner | Glass Care | Tire/ Rim Care | Interior Trim/ Dashboard | Leather
Silicone oils |  |  | X | X |  | X | X | X
Silicone emulsions |  |  | X | X |  | X | X | X
Aminofunctional silicones (oils/emulsions) |  |  | X | X | X | X | X | 
Alkyl Aryl silicones |  |  |  | X |  |  | X | 
Volatile silicones |  |  | X |  |  | X |  | 
Silicone glycols |  |  |  |  | X |  | X | X

## Slide 42: Home care – product selector guide
Product | Water based | Solvent based | Leather Care | Furniture Care | Hard Surface Care | Glass Care
Silicone oils |  |  | X | X |  | 
Silicone emulsions |  |  | X | X | X | X
Volatile silicones |  |  | X | X |  | 
Silicone glycols |  |  |  | X | X | X
Aminofunctional silicones (oils/emulsions) |  |  | X | X | X | X
Silicone resins |  |  | X | X |  | 
Antifoams |  |  |  |  | X | 

## Slide 43: Customer support
Formulation support
We can provide examples of formulations using our silicones
Ready-to-use products
BRB PTFE Clean & Shine
Polish for 2nd hand cars (abrasive)
BRB New Car Polish
Polish for new cars (mild)
BRB Glass Water Repellant
Windscreen polish
BRB Cockpit Shine
Dashboard polish

## Slide 44: Laundry Care – product range
Silicone antifoams
  BRB Akasil TG 10/20/30
  BRB Akasil RE 20
  BRB Akasil 20LD
Silicone Glycols
  BRB 526
Silicone Emulsions
  BRB Sempure 35, BRB Sempure 60
  BRB Sempure 3733
  BRB Sempure 270
Volatile Silicones
  BRB CM 50

## Slide 45: Laundry Care – specific applications
Silicone antifoams
  Foam control in liquid detergents & fabric conditioners
  Antifoam systems for powder detergents (post-addition or spray on)
Silicone Glycols
  Wetting agent, ease of ironing benefit in liquid laundry tablets
Silicone Emulsions
  Softness, anti-wrinkle, ease of ironing and water absorbency for fabric softeners
Volatile Silicones
  Dry cleaning solvent

## Slide 46: BRB Akasil 20LD – for Laundry Care
Properties
  20% active, high performance, silicone based antifoam emulsion
  Optimized for use in surfactant-rich formulations and environments, as encountered in the detergent and textile industries
Benefits
  • Effective and durable over a wide pH range
  • Outstanding reliability and versatility
  • Suitable for products with high salinity
  • Available in easy-to-use emulsion form
  • Good high temperature performance
  • Excellent knockdown as well as defoaming performance.

## Slide 47: BRB Sempure 270 – for Laundry Care
Properties
  70% active, micro-emulsion of quat polyether terpolymer
  Specifically developed for fabric treatment
  Recommended for use in rinse-cycle laundry products
  Compatible with organic softeners (e.g. esterquats)
  Typical formulation contains 2.5% BRB Sempure 270 and 15% organics
  Post-addition with moderate agitation
Benefits
  Deposits onto fabric from the rinse cycle
  Enhance softness (silicones have a silky feel attenuating the ‘greasier’ organics)
  Promotes ease ironing
  Improve water absorbency

## Slide 48: Laundry Care – product selector guide
Product | Liquid laundry detergent | Liquid laundry tablets | Powder laundry detergents | Fabric softeners | Dry Cleaning
BRB Akasil TG 10, 20, 30 | X |  |  | X | 
BRB Akasil RE 20 | X |  |  |  | 
BRB Akasil 20LD | X |  |  |  | 
BRB 526 |  | X |  |  | 
BRB Sempure 35 & 60 |  |  |  | X | 
BRB Sempure 3733 & 270 |  |  |  | X | 
BRB CM 50 |  |  |  |  | X